# Indexing XRD-patterns, getting cell parameters

Armel Le Bail

Université du Maine, Laboratoire des Oxydes et Fluorures, Avenue O. Messiaen, 72085 Le Mans Cedex 9, France - Email : alb@cristal.org - Web : http://www.cristal.org/

## Abstract

Some keys, hints and tips for the successful indexing of a powder diffraction pattern are given through examples, by using exclusively free access programs for academic research. Essentially, the sample has to correspond to a single phase; the powder pattern resolution should be maximal, avoiding preferred orientation; the tools used for peak position hunting and indexing should be the best on the market; the figures of merit have to be understood so as to be able to save time by discarding the poor quality suggestions of the indexing programs; further checking by post-indexing visualization is recommended in case of good quality multiple equivalent propositions; finally, whole pattern fitting has to be the ultimate test in order to be convinced enough for attempting the structure solution.

Tip-1 : Indexing powder diffraction data is probably the crystallography topic where the traditional way of sharing openly computer programs remains the more respected (ITO, TREOR, DICVOL, CRYSFIRE, McMaille, etc).

## Exercise 1 – starting with a simple case : Y2O3

The powder pattern for that exercise is available at http://www.cristal.org/powbase/ (Powbase is a small database of powder pattern), as well as the others.

Start WinPLOTR, select “File”, then select “Open pattern file”, select INSTRM=0 in the list of “Format of data file”, a windows allows you to select the data, find y2o3.dat (inside of 81.zip in PowBase) and open it.

Tip-2 : The file y2o3.dat is a text file. Lines starting by ! or # are ignored by WinPLOTR. The data format corresponding to INSTRM=0 corresponds to a line with starting angle, step and last angle in degrees 2, then follow the intensities step by step in free format :

15.00 0.01 145.90

25        22        19        21        19        14        23        25

26        21        24        22        33        26        15        21

19        20        20        16        14        17        22        21

17        27        18        30        21        21        21        18

19        22        22        28        19        19        13        30

………..etc

37        33        44        48        55        46        61        48

64        53        72        80        87       122       150       142

150       203       238       256       316       386       453       557

695       762       918      1005      1263      1372      1416      1398

1363      1242      1095      1027       837       761       587       506

384       300       205       199       158       121       123       109

107        82        64        67        42        68        62        59

55        51        45        47        36        31        31        43

32        28        39        27        22        35        25        29

29        17        23        24        18        23        26        29

At this stage you are expected to make use of your crystallography expertise already. You must answer to the question : high or low symmetry ? Clearly, just by looking at the pattern, there are evidences for a high symmetry because of the quasi constant angular interval between the peak positions. Keep that possibility in mind.

Then click on “Points selection”, and “Automatic peak search”, select “Search Cu K1 K2 doublets” (yes, this is conventional laboratory X-ray data without any monochromator in the incident beam). Click on “OK”, the result is 21 peaks found if the range goes up to 93°(2). Clearly, many peaks with small intensity were not identified.

Go back to “Points selection”, and “Automatic peak search”, and change the “peak threshold” to 0.005 instead of 0.02, click on OK, that time 38 peaks are detected, click OK. Even if some very small peaks are not taken into account, we can try now to index.

Click again on “Points selection”, then on “save as”, then on “Save points for McMaille” (what were you expecting, I am the author of McMaille ;-):

Then a box is opened, type a title (why not Y2O3), give the wavelength (1.54056, yes this is K1 only now) and let the zeroshift to be 0, click OK, the program says that a file named  y2o3_mcmy.dat has been created, click OK and quit WinPLOTR.

Here is the y2o3_mcmy.dat file content :

Y2O3

! Wavelength, zeropoint and NGRID (NGRID=3: black box mode)

1.540560   0.000  3

! List of 2theta positions, intensity (min.=20)

20.50481    1411.71155

29.15784   11198.95700

33.79123    2632.66553

35.91046     531.02966

37.92135     135.21042

39.84880     606.23480

41.70092     118.49068

43.48877     881.15845

46.88918     271.40564

48.52835    4213.47021

50.12016     230.08562

51.68559      66.62399

53.20726     506.43854

54.69715     117.27492

56.16987     404.76215

57.61465    2603.39868

59.03540     563.80334

60.43375     471.21359

61.81146     194.23712
      Etc

Copy that file inside of the directory where McMaille is installed and start this indexing program (click on “McMaille.exe, and give the file name without extension: y2o3_mcmy) :

Tip-3 : You will probably not obtain exactly this result, because McMaille uses a Monte Carlo algorithm, implying a sequence of pseudo-random number. You would obtain the same result if you start exactly at the same point in that sequence. The starting point is defined in McMaille by the time (expressed in seconds since the beginning of the day) at the instant when you start the program. At least you should obtain a similar result in a different order.

Let us comment these results. McMaille is working in the so-called “black box mode”. We have given only very few informations : peak positions, intensities, wavelength, a null zeropoint (this is a constant – an approximation - angular shift due to both instrumental – if misaligned - and sample – if not in the diffracting plane – effects that we should not neglect in the next exercises). In that black box mode, McMaille follows its own strategy : testing first the highest symmetries, down to triclinic, inside of some predetermined limits of cell parameters and volumes.

Tip-4 : All indexing programs have such maximal default values which the user has to know – see the manuals - and should modify if no result is obtained.

The essential things to see in the output file of any indexing program are the FoMs (Figures of Merit), generally noted M20 and F20 or F30. The higher are these FoMs, the more the corresponding cells are plausible. For the definitions of the FoMs, see the excellent chapter 7, autoindexing, written by Per-Erik Wernet in the book “Structure Determination from Powder Diffraction Data.

Tip-5 : References are at the end of the tutorial

McMaille provides also these FoMs for selected good cells, but the solutions are sorted according to a somewhat different criterion noted Rp which is equivalent to a Rietveld profile reliability. The program will not always stop like it has done here, it may well examine all symmetries down to triclinic. In black box mode, it will stop if a solution with Rp < 0.02 is found. In that case, it has found an orthorhombic solution with Rp = 0.013 with a very small cell volume (149 Å3) and very large conventional FoMs (M20 = 280). A very small Rp value (< 0.05) means that the powder pattern is well fitted, the smaller will be Rp, the larger will be the conventional FoMs M20 and F20.

But is it the good cell ?

Tip-6 : The ultimate decision has to be made by the user, always…

Having a good formation in crystallography will help a lot to make the decision. In that case, solutions with small Rp are also proposed in cubic (R = 0.032), hexagonal (R = 0.038) and tetragonal (R = 0.023).

Tip-7 : First important point to keep in mind for becoming an expert in indexing : any cell with a high symmetry can also be indexed in all the lower symmetries.

In that case, if McMaille had not stopped at the orthorhombic symmetry, it would have provided cells also in monoclinic and triclinic symmetries, possibly with even lower Rp values.

Are all lines indexed ? In black box mode, whatever the number of lines given, McMaille will work only by using the first 20 lines, and has a tolerancy of 3 unindexed lines. The number of not indexed lines is provided (parameter Nind in the figure above). All lines are indexed in cubic, tetragonal and orthorhombic (Nind = 0). Making the ratio Vcubic/Vortho gives 1192/148 = 8… So, very probably, the cell is cubic. McMaille prepares a new .dat file for further investigations in manual mode. That file name is y2o3_mcmy-new.dat. Edit that file :

Y2O3

! Wavelength, zeropoint, Ngrid

1.540560 0.0000 0

! Codes for symmetry

1 0 0 0 0 0                                     Cubic only

! W, Nind

0.300  3

!Pmin, Pmax, Vmin, Vmax, Rmin, Rmax, Rmaxref

2. 20. 8. 2000. 0.05 0.25 0.50                 Decrease some values here

! Ntests, Nruns

2000 1

!  2-theta   Intensity

20.50481       1411.712

29.15784       11198.96

33.79123       2632.666

35.91046       531.0297

37.92135       135.2104

39.84880       606.2348

41.70092       118.4907

43.48877       881.1584

46.88918       271.4056

48.52835       4213.470

50.12016       230.0856

51.68559       66.62399

53.20726       506.4385

54.69715       117.2749

56.16987       404.7621

57.61465       2603.399

59.03540       563.8033

60.43375       471.2136

61.81146       194.2371

63.17843       149.1199

64.53022       288.8621

65.85427       145.6454

69.78623       190.6706

If you read the manual (don’t believe you can become an expert in 2 hours…) you will see that that file is configured for a search only in cubic, just fine, this is what we want to do. Apply again McMaille to that file :

Have a look inside of the y2o3_mcmy-new.imp file containing the detailed results :

FINAL VALUES   : (STANDARD DEVIATIONS : 2nd LINE)

ZERO    LAMBDA      A        B        C      ALPHA     BETA    GAMMA

-0.014    1.5406  10.6059  10.6059  10.6059   90.000   90.000   90.000

0.001    0.0000   0.0003   0.0003   0.0003    0.000    0.000    0.000

RECIPROCAL CELL :   0.09429  0.09429  0.09429   90.000   90.000   90.000

VOLUME (A**3)  :     1193.017

H     K     L  TH(OBS)    TH-ZERO    TH(CALC)     DIFF.

2     1     1    20.505     20.491     20.495     -0.004

2     2     2    29.158     29.144     29.143      0.001

4     0     0    33.791     33.777     33.777      0.000

4     1     1    35.910     35.897     35.893      0.003

4     2     0    37.921     37.907     37.907      0.001

3     3     2    39.849     39.835     39.833      0.002

4     2     2    41.701     41.687     41.685      0.002

4     3     1    43.489     43.475     43.472      0.003

5     2     1    46.889     46.875     46.881     -0.006

4     4     0    48.528     48.514     48.515     -0.001

4     3     3    50.120     50.106     50.110     -0.003

4     4     2    51.686     51.672     51.668      0.004

6     1     1    53.207     53.193     53.193      0.000

6     2     0    54.697     54.683     54.688     -0.005

5     4     1    56.170     56.156     56.157     -0.001

6     2     2    57.615     57.601     57.600      0.001

6     3     1    59.035     59.022     59.021      0.001

4     4     4    60.434     60.420     60.421     -0.001

7     1     0    61.811     61.798     61.801     -0.004

6     4     0    63.178     63.165     63.165      0.000

6     3     3    64.530     64.516     64.511      0.005

6     4     2    65.854     65.840     65.843     -0.003

7     3     2    69.786     69.772     69.761      0.011

8     0     0    71.059     71.045     71.044      0.001

5     5     4    72.331     72.318     72.318      0.000

8     2     0    73.591     73.577     73.582     -0.006

6     5     3    74.859     74.845     74.839      0.006

6     6     0    76.097     76.083     76.087     -0.004

7     4     3    77.347     77.333     77.330      0.004

6     6     2    78.580     78.566     78.566      0.000

8     4     0    81.036     81.022     81.023      0.000

8     3     3    82.255     82.241     82.244     -0.003

8     4     2    83.480     83.466     83.463      0.003

6     5     5    84.689     84.675     84.678     -0.004

7     5     4    87.115     87.101     87.102     -0.001

7     6     3    89.529     89.515     89.521     -0.006

8     4     4    90.747     90.733     90.730      0.003

9     4     1    91.955     91.941     91.940      0.001

M(20) =    168.09

F(20) =    151.03 (  0.0021,  62)

This looks extremely good.

Will any attempt be that easy ? Certainly not… this was the first exercise and you are lucky.

McMaille prepares a file for a Rietveld-like fit (a .prf file) for the best solution which you can see by using WinPLOTR. Let us see that y2o3_mcmy-new.prf file. Start WinPLOTR, click on “File”, then on “Open Rietveld/profile file”, select “101 : Fullprof PRF file”, click on OK, and select the file in the Windows box.

The vertical bars note all lines that should be there. A lot are lacking. You may realize, by examining the hkl indices of the indexed lines that there is a systematic relation h + k + l = 2n, and thus the Bravais lattice is very probably I – centered. McMaille will not do that automatically for you.

Tip-8 :  Some programs perform automatically everything (indexing, space group suggestion, solving the structure, refining, etc), like EXPO2006 : use these programs first, and if they fail, go back to some standalone programs.

Tip-9 : Only solving the structure confirm the indexing… but this is not the scope of this tutorial.

Tip-10 : you should never try to index without having defined the zeropoint…

Exercise 2 – A bit more difficult : -AlF3

Software for hunting the peak positions are numerous (see session 2 of the SDPD Internet Course : http://sdpd.univ-lemans.fr/DU-SDPD/), free access (WinPLOTR, PowderX, EXPO2004, etc) or commercial (EVA, Highscore, Jade, etc). Let us try PowderX on the 
-AlF3 powder pattern. In fact the pattern is corrected for a large zeropoint error (0.3° !) due to the fact that the sample was dusted on the sample holder for avoiding preferred orientation.

Tip–11 : Dusting a sample on the holder through a sieve allows for reducing preferred orientation effects. But since this enlarges the peak width, it is not recommended at the indexing stage : press the sample for a better resolution.

Tip-12 : Typical excellent minimal FWHMs (Full Width at Half Maximum) are (for well crystallized compounds) : 0.04 to 0.06°(2) for conventional laboratory instrument and 0.005 to 0.01°(2) for third generation synchrotron source. Note that a 0.02° FWHM at a synchrotron source with a 0.7 Å wavelength is equivalent to 0.04° in your lab with a copper target…

Tip-13 : The zeropoint correction can be done before indexing by two methods : mixing a reference compound with the sample or using the harmonics technique. Let us consider that you know how doing these “simple” things.  If not, see sessions 2 and 3 of the SDPD Internet Course.

The -AlF3 powder pattern is also available in PowBase (1.dat inside of 1.zip), and can be read with PowderX by clicking on “File”, then “Import Data”, then “RIET7” for the format. This is a format analogous to the one read by WinPLOTR  (INSTRM=0), but you have to add 4 header lines (blank if you wish). First remove the background : click on “Substract Background” then on “Show” in the small box and the on “OK” if you are satisfied (otherwise play with the options, and zoom to see the effect).

Click on “Alpha2 Elimination”, click on “Test”, click on “Finish”.

Click on “Peak Search”, then on “Show”, modify the intensity limit for the detection of the weakest peaks if you wish, then click on OK.

Save the file after confirmation of the wavelength :

2Theta     d (A)    Height      Area     FWHM

12,292   7,19449     336,0    1262,2    0,0800

15,040   5,88588   18391,1  147126,3    0,1600

17,358   5,10448   19047,3  144454,3    0,1600

21,324   4,16331   47804,6  323420,4    0,1400

23,056   3,85441   38529,0  268961,3    0,1400

24,656   3,60768   11816,5   82581,7    0,1400

25,039   3,55334    5890,4   54511,0    0,2000

26,272   3,38940   28732,0  227980,7    0,1600

26,632   3,34432     408,5    1447,7    0,0800

26,748   3,33017     290,9    1085,7    0,0800

27,634   3,22529   52845,1  474146,2    0,1800

27,936   3,19114     644,3    2064,0    0,0800

29,023   3,07407   25452,0  203382,7    0,1600

29,240   3,05179     943,2    3265,4    0,0800

29,401   3,03544     284,2    1420,5    0,1000

29,729   3,00260     337,7    1909,7    0,1200

30,394   2,93842    8950,3   71150,3    0,1600

34,038   2,63177    1399,2   11181,9    0,1600

35,239   2,54473     698,6    4946,1    0,1600

36,355   2,46914    1346,2   10729,8    0,1600

37,523   2,39493    1679,4   12700,5    0,1600

39,501   2,27942    2415,3   16903,5    0,1400

40,567   2,22199    3282,1   22194,2    0,1400

41,526   2,17285    1868,9   14926,1    0,1600

Tip-14 : You may also play with the zeropoint correction system inside of PowderX. Then save the file for TREOR and transform it into a file for McMaille ;-). You have to change the comma into points and remove the stuff at the end of the file, rename it as AlF3.dat in the McMaille directory.

Tip-15 : When using PowderX, be carefull that the wavelength was taken into account, otherwise use only 2 values, but not d(Å) values.

AlF3

1.54056   0   3

12.292          6

15.040        348

17.358        360

21.324        905

23.056        729

24.656        224

25.039        111

26.272        544

26.632          8   Remove

26.748          6   Remove

27.634       1000

27.936         12

29.023        482

29.240         18

29.401          5   Remove

29.729          6   Remove

30.394        169

34.038         26

35.239         13

36.355         25

37.523         32

39.501         46

40.567         62

41.526         35

43.515         36

44.450        195

44.727          8   Remove

46.241        145

46.523         10

47.176        251

47.480          9   Remove

49.878         38

Remove those weak peaks with intensity < 1% of the most intense one (maybe leaving the first at low angle).

Tip-16 : Peaks at low angles are essential even if they are weak.

Start McMaille and see the results. Cells with R close to 5% appear in tetragonal, orthorhombic, monoclinic, you may stop the calculation by typing K (large character), and then think…

Which cell is the good one ? Again there are several possibilities. Remember that any high symmetry cell can be proposed in a lower symmetry. In that case, the tetragonal cell with smallest volume seems to have chances to be the correct one. McMaille produces files with .ckm extension which can be read by the Chekcell program and may help to decide.

The AlF3.ckm file :

N   FoM     V           V/V1

17   93.28    374.247  1.00                                     7.1866  10.2015   5.1047  90.000  90.047  90.000

17   87.55    748.954  2.00                                   10.2023  10.2141   7.1872  90.000  90.000  90.000

17   87.52    379.961  1.02                                     5.1844  10.1684   7.3235  90.000 100.212  90.000

17   86.81    374.340  1.00                                   11.4104   7.1869   5.1053  90.000 116.603  90.000

18   86.00    379.919  1.02                                     5.1843  10.1677   8.1882  90.000 118.331  90.000

17   85.14    374.347  1.00                                   10.2026   7.1867   5.1054  90.000  90.030  90.000

18   84.59   1123.379  3.00                                  15.3210   7.1867  10.2026  90.000  90.000  90.000

17   83.63    374.484  1.00                                     5.1070   7.1872  10.2025  90.000  90.000  90.000

17   82.55    502.511  1.34                                     7.6607  10.1696   6.8487  90.000 109.642  90.000

17   80.76    308.628  0.82                                     4.2084  10.2036   7.8445  90.000 113.620  90.000

17   80.52    441.141  1.18                                     7.3487  10.1996   6.0087  90.000 101.627  90.000

17   79.36    308.588  0.82                                     4.2083  10.2022   7.2651  90.000  98.381  90.000

17   76.28   1119.785  2.99                                  12.4887   8.7879  10.2032  90.000  90.000  90.000

17   75.64    354.395  0.95                                     7.2113  10.2017   4.8337  90.000  94.722  90.000

17   75.53    338.952  0.91                                     4.6103  10.2002   7.3041  90.000  99.319  90.000

19   75.35   1831.669  4.89                                   14.3750  12.4897  10.2020  90.000  90.000  90.000

17   74.57    338.922  0.91                                      7.9813  10.1991   4.6105  90.000 115.436  90.000

17   73.60    502.352  1.34                                      7.6535  10.1970   6.8273  90.000 109.471  90.000

17   72.48   2995.752  8.00                                   14.4370  14.4370  14.3732  90.000  90.000  90.000

20   72.46   2995.731  8.00                                   10.2086  10.2086  28.7457  90.000  90.000  90.000

18   68.96    336.200  0.90                                     7.9158  10.2015   4.5834  90.000 114.722  90.000

18   68.34    371.538  0.99                                    10.1685   5.1044   7.1584  90.000  90.522  90.000

19   67.56   1208.311  3.23                                    14.2227  10.2029   8.3267  90.000  90.000  90.000

18   67.31    470.527  1.26                                     6.4170  10.2025   7.4635  90.000 105.645  90.000

17   64.36    429.930  1.15                                     7.2975  10.2033   5.8628  90.000  99.978  90.000

17   63.96    362.825  0.97                                     4.9471  10.2019   7.1966  90.000  92.649  90.000

17   63.92    748.935  2.00                                    10.2085  10.2085   7.1865  90.000  90.000  90.000

17   63.25    338.099  0.90                                     7.3083  10.1965   4.6008  90.000  99.549  90.000

Most of the cells with the highest FoMs have volumes multiple of 374 Å3.

Start Chekcell. Click on “File”, then “Open”, then “Diffraction Data File”, then “Rietveld Format”, specify the wavelength when asked by the program, the pattern should appear (the data file must have 4 header lines), zoom eventually.

Then, open the .ckm file : click on “File”, “Open”, “Cell File”, “Crysfire Summary File”, search for the .ckm option and select it, find AlF3.ckm (note that sub-files for different symmetries are also built up by McMaille) :

There is a chance that the cell would be tetragonal with cell parameters a = 10.2 and c = 7.2 Å. One intense impurity line is obvious (this is -AlF3).

Tip-17 : Whole profile fitting (Pawley of Le Bail methods) would provide the ultimate convincing arguments (a perfect fit…) and allow to decide for some space group possibilities.

Exercise 3 – C28H24O8 synchrotron data - Even more difficult ?

The powder pattern for that sample is also inside of PowBase (see 89.dat in 89.zip). Let us come back to WinPLOTR for the peak position extraction. Wavelength :  = 1.15023 Å.

Tip-18 : in principle, synchrotron data corresponds to parallel beamline so that there is no zeropoint. In practice, but verify…

Use the automatic peak search option as in the exercise 1, decrease the peak threshold to 0.005 in order to locate some of the weakest peaks and save the file for McMaille :

Start McMaille, and during the calculations, save also the results for TREOR :

Do not forget to change the wavelength and increase the limit of the FoM to 50 : this is synchrotron data, you may expect high FoMs.

! DATA FILE: 89.dat

! INSTRM:  0

C28H24O8

4.98193    3286.80762      83.30889

9.99003    1472.15564      57.64410

11.83465    4172.48730      66.85038

14.26077    5120.27832     132.29897

14.54244    2541.02197     127.71822

14.68000    2377.54810     114.03048

15.01395    1603.88196      96.83777

15.67321     402.99741     105.96571

16.43242     187.91476     106.60686

18.40516     320.04770     157.74744

18.57075   10253.10740     161.52725

18.81269     205.76633     155.59302

20.06825     933.78021     125.71569

21.49577    1768.68835     149.90627

21.70489    2902.25244     157.81589

21.89608     637.32843     155.65938

22.13791    1497.10925     137.45313

22.80752     548.14728     116.36189

22.90763     345.16406     117.80325

23.72424     243.58403     108.58457

24.44472     301.27338      99.54028

24.98247     252.92178      90.35323

26.37432     219.01628      82.18118

28.60269     157.93480      75.28192

28.76217     303.62329      73.10251

29.97874     350.80719      71.17887

30.52339     490.87183      83.80813

30.69416     222.56485      81.57237

32.01038     431.36816      96.65090

32.23336     385.18842      92.53907

32.98502     394.52618      82.19423

33.36611     675.33411      80.25625

33.97608     144.84073      73.54704

CHOICE=3,

WAVE= 1.15023,

MONO=125.00,

VOL=  1500.,

CEM=  20.,

MERIT= 50.,

END*

Maybe there are too much data.

Tip-19 : generally, the first 20 lines of a powder pattern are sufficient for indexing. Using more may even obscure the results…

And run TREOR inside of WinPLOTR :

Inside of WinPLOTR, TREOR  produces also files for CHEKCELL.

Tip-20 : the statement ***** YOU HAVE GOT AN INTERESTING RESULT !!!  ***** is given only if M(20) is better than your specifications, generally it announces a correct solution.

Tip-21 : TREOR runs much faster than McMaille… It is better to apply it first.

Now go back to the McMaille screen, and stop the calculations by typing K (capital letter). Maybe it had enough time to find that monoclinic solution as well ?

## Exercise 4 – Tetracycline Hydrochloride – Synchrotron data

Use the file tetrasync.dat in PowBase (download 17.zip) with wavelength :  = 0.692 Å. This is a capillary measurement (explaining the amorphous component).

Let us try again WinPLOTR :

Let us save the data for DICVOL04 :

Tip-22 : DICVOL04 is generally much faster than McMaille but is a bit longer than TREOR for low symmetries (monoclinic and triclinic), in general, so, start with TREOR, then DICVOL04, then McMaille, then CRYSFIRE.

Tip-23 : Using first TREOR and DICVOL can be sufficient and convincing enough for not applying any other indexing software.

# Input file for WDICVOL04 (created by WinPLOTR)

# created by WinPLOTR: 22-05-2006  at 14:40:39

! DATA FILE: tetrasync.dat

! INSTRM:  0

Tetracycline Hydrochloride

20   2   1   1   1   1   1   0                      ! N,ITYPE,JC,JT,JH,JO,JM,JTR

25.0  25.0  25.0 0.0   2500.0  90.0 125.0  ! AMAX, BMAX, CMAX, VOLMIN, VOLMAX,

BEMIN, BEMAX

0.69200    0.000    0.000    0.000              ! WAVE,POIMOL,DENS,DELDEN

0.030   20.000   3   0   1   1    ! EPS,FOM, N_IMP, ZERO_search, ZERO_refinement, ISUP

3.98593   36431.48050   10162.20610

4.40658   41888.94530   10565.47270

4.75146   29037.62700   11002.17770

5.04268   65646.02340   11368.10350

5.38045   33498.84770   11182.45120

5.91553   28324.10940   11602.85940

6.20306   50488.21090   12065.03910

6.67000   17883.95510   12214.81350

6.93070   43182.59770   13354.95020

7.15491   77665.66410   13321.50490

7.58623   38302.71090   13787.45120

7.97693   15808.31350   14298.10740

8.25668   41806.14060   14822.07620

8.75711   36411.66410   17468.19530

8.93881   53459.96480   17769.21090

9.34233   49226.54300   18679.95310

9.51136   26989.77340   19966.95310

9.60437   35311.25780   20394.47270

9.77657   29438.52150   20606.06640

9.84160   42509.96090   20488.37500

10.09644   24946.23630   19272.28520

10.26473   24402.79490   19494.67380

10.42091   38604.35940   20171.22270

10.55440   22594.34180   20487.28520

10.76932   39757.06250   20055.43360

10.91930   46911.87110   20154.14650

11.16057   33845.78910   20396.83400

11.97332   29695.01560   19972.38870

12.16527   41121.92190   20340.83790

Try also with TREOR and McMaille.

Go back to previous exercises and try the programs that were not already applied. Paly with Chekcell.

Tip-24 : A simple way to deal with large cells without changing the default values of the indexing program is to give a fictitious wavelength being 2, 5 or 10 times (proteins) smaller than the real one. Then, the obtained cell parameters will be 2, 5 or 10 times smaller that the effective ones.

## Additional notes

Not obtaining results with TREOR, DICVOL04 or McMaille, you may consider trying with CRYSFIRE (see session 3 of the SDPD Internet Course, or the CCP14 Web site). Consider also to use N-TREOR (either standalone or inside of EXPO2004) instead of TREOR. Visit the Indexing Benchmarks Web pages comparing the performances of many indexing programs, and see why using ITO may not be very interesting.

## References

Useful Web address :

CCP14 : http://www.ccp14.ac.uk/

Indexing Benchmarks : http://sdpd.univ-lemans.fr/uppw/benchmarks/

SDPD Internet Course : http://sdpd.univ-lemans.fr/DU-SDPD/

Most recent review papers about indexing :

P.-E. Werner in “Structure Determination from Powder Diffraction Data”, Edited by W.I.F David, K. Shankland, L.B. McCusker and Ch. Baerlocher, Oxford Science Publications, Chapter 7 : “Autoindexing”, 2002, 118-135.

R. Shirley, “Overview of powder-indexing program algorithms (history and strenghts and weaknesses). IUCr Computing Commission Newsletter 2 (2003) 48-54.

J. Bergmann, A. Le Bail, R. Shirley and V. Zlokazov, “Renewed interest in powder diffraction data indexing”, Z. Kristallogr. 219 (2004) 783-790.

Programs :

Chekcell : J. Laugier & B. Bochu, http://www.inpg.fr/LMGP (and CCP14)

CRYSFIRE : R. Shirley, “The Crysfire 2002 system for automatic powder indexing: user’s manual. Lattice Press: Guilford, UK (2002).

DICVOL04: A. Boultif & D. Louër, “Powder pattern indexing with the dichotomy method”, J. Appl. Crystallogr. 37 (2004) 724-732.

McMaille : A. Le Bail, “Monte Carlo indexing with McMaille”, Powder Diffraction 19, 2004, 249-254. http://www.cristal.org/McMaille/

N-TREOR : A. Altomare, C. Giacovazzo, A. Guagliardi, A.G.G. Moliterni, R. Rizzi & P.-E. Werner,“New techniques for indexing : N-TREOR in EXPO”, J. Appl. Crystallogr. 33 (2000) 1180-1186.

PowderX : C. Dong, “PowderX: Windows-95-based program for powder X-ray diffraction data processing”, J. Appl. Crystallogr. 32 (1999) 838.

TREOR: P.-E. Werner, L. Eriksson & M. Westdahl, “TREOR, a semi-exhaustive trial-and-error powder indexing program for all symmetries”, J. Appl. Cryst. 18 (1985) 367-370.

## WinPLOTR : T. Roisnel & J. Rodriguez-Carvajal,

## http://www-llb.cea.fr/fullweb/winplotr/winplotr.htm