QUESTIONNAIRE FOR STRUCTURE DETERMINATION BY POWDER

DIFFRACTOMETRY ROUND ROBIN

Submitted by

S. Wilke, M. A. Neumann, G. E. Engel, F. J. J. Leusen

Molecular Simulations Ltd, 230/250 The Quorum, Barnwell Road, Cambridge CB5 8RE,

England

Only the solution of the second sample has been attempted. The quality of the

experimental data is sufficient to solve the crystal structure.

1. Preliminary work

1.1 Did you obtain additional information from the chemical formula ?  No

Remark: The molecular formula was taken from transparency 30 of A. Le Bails talk on

trends in SDPD (http://www.cristal.org/iniref/ecm18/t30.gif)

1.2 Did you obtain additional information from the powder pattern ?  Yes

The program Powder Fit was used to determine accurate lattice parameters, profile

parameters and background coefficients from the synchrotron powder pattern. Powder Fit

is part of the Cerius2 software package.

1.3 Did you extract the structure factors ?  No

2 Structure solution

2.1 Did you use direct methods ?  No

2.2 Did you use Patterson methods ?  No

2.3 Did you use another method ?  Yes

2.3.1 If yes, which method(s) ?

The structure was solved using a direct space approach and a Monte Carlo/simulated

annealing method. Molecules are treated as rigid bodies with a limited number of internal

torsional degrees of freedom. The quality of the model structure is determined by a full

profile comparison with the experimental powder diffraction pattern. Minima of the Rwp

factor are located by rigid body Rietveld refinement, thus allowing for relatively high

temperatures in the simulated annealing procedure.

In a first step, the structure was solved with a total of 11 degrees of freedom. The initial

temperature was chosen high enough to overcome all barriers on the Rwp hypersurface.

The comparison with the synchrotron powder pattern was carried out in the angular range

from 2.12 to 17, covering a total of 133 reflections. Hydrogen atoms were ignored in

the calculation of the peak intensities. The best Rwp factor obtained had a value of 6.04%

(All cited Rwp values have been calculated without background subtraction.).

In a second step, the solution was improved by searching the Rwp hypersurface in the

vincinity of the minimum located in the first step. For this purpose, some of the

intramolecular bonds were cut and the numbers of torsional degrees of freedom was

increased. A Monte Carlo/simulated annealing run at low temperature with a small Monte

Carlo step width and a total of 27 degrees of freedom resulted in an Rwp factor of 2.87%.

The comparison with the experimental powder spectrum was performed for the full

angular range from 2.12 to 40.0. Hydrogen atoms were now taken into account in the

calculation of the diffraction intensities.

2.3.2 Which program(s) did you use ?

The structure was solved using the program Powder Solve, implemented in the Cerius2

software package.

2.4 Did you first locate the whole structure  Yes

2.4.3 Was the initial model derived from the molecular formula ?  Yes

The initial molecular geometry was derived from the molecular formula by force field

and semi-empirical calculations. Energy minimisations were carried out using the

Dreiding 2.21 force field, the COMPASS force field and the PM3 hamiltonian, leading to

three different starting geometries. The crystal structure was solved with the result of the

Mopac PM3 calculation as a starting point.

2.4.4 Were the initial atomic coordinates taken from a known structure ?  No

3 Structure completion

Since the whole structure was located in the structure solution step, structure completion

was not necessary.

4 Final refinement

Three alternations of rigid body Rietveld refinement and lattice energy minimisation

were used in the final refinement step. The rigid body refinement was carried out with

Powder Solve using 5 rigid bodies with a total of 11 internal torsional degrees of

freedom. The lattice energy minimisations based on the COMPASS forcefield were

limited to a small number of minimisation steps, thus assuring a compromise between a

low Rwp factor and reasonable bond lengths and bond angles. The last Rietveld

refinement step produced a Rwp factor  of 2.42%. The subsequent lattice energy

minimisation was stopped when the Rwp factor reached a value of 2.67%. Finally, the

hydrogen bonded network was analysed. Some of the torsion angles defining the

orientation of the OH groups were slightly adjusted to obtain a more favorable orientation

for hydrogen bonding. This modification led to a final Rwp factor of  2.70% (Rp=2.0%).

At the present stage, Powder Solve does not allow the refinement of thermal parameters

and the calculation of standard deviations. All thermal parameters were set to zero. The

following atomic coordinates were obtained:

NAME       X          Y          Z

C1    0.66562    0.12218   -0.39185

C2    0.56719    0.19782   -0.37715

C3    0.46574    0.16839   -0.32059

C4    0.48365    0.07626   -0.26126

C5    0.52054   -0.01593   -0.31407

C6    0.62879    0.01030   -0.37581

C7    0.36954    0.05111   -0.20873

C8    0.29390   -0.03113   -0.22477

C9    0.31668   -0.11241   -0.29584

C10   0.41303   -0.07088   -0.35872

C11   0.18122   -0.04754   -0.17332

C12   0.10320   -0.13919   -0.19698

C13   0.10974   -0.18298   -0.27782

C14   0.19814   -0.13769   -0.34321

C15   0.01895   -0.17597   -0.13737

C16  -0.05442   -0.26014   -0.15697

C17  -0.04676   -0.30567   -0.23637

C18   0.03382   -0.26669   -0.29641

C19   0.21009   -0.21028   -0.42090

C20   0.56525    0.29162   -0.41612

C21   0.80850   -0.01680   -0.27748

C22   0.71608   -0.16433   -0.36146

O1    0.00132   -0.13085   -0.05839

O2    0.15712   -0.04022   -0.37577

O3    0.14787    0.01176   -0.11693

O4    0.34471    0.11668   -0.14195

O5    0.36794    0.21544   -0.31471

O6    0.58297    0.10232   -0.20556

O7    0.76187    0.13836   -0.42857

O8    0.46541    0.35105   -0.41288

N1    0.65508    0.33576   -0.46066

N2    0.74387   -0.05052   -0.35670

H1    0.21760   -0.29338   -0.40522

H2    0.28773   -0.19002   -0.46189

H3    0.12884   -0.20105   -0.46095

H4    0.08807   -0.05209   -0.41011

H5   -0.12044   -0.28934   -0.11047

H6   -0.10801   -0.37029   -0.25207

H7    0.40524    0.11026   -0.09822

H8    0.36758   -0.02116   -0.40665

H9    0.85330    0.05789   -0.29099

H10   0.87622   -0.07639   -0.26248

H11   0.74397   -0.00888   -0.22490

H12   0.80114   -0.20787   -0.35462

H13   0.67468   -0.17899   -0.42401

H14   0.65168   -0.18541   -0.31133

H15   0.47828    0.41115   -0.44744

H16   0.65055    0.40842   -0.48355

H17   0.55624    0.09247   -0.14730

H18   0.03362   -0.30295   -0.35968

H19   0.03105   -0.06157   -0.06244

H20   0.54873   -0.07041   -0.26385

H21   0.35283   -0.18457   -0.26691

H22   0.44976   -0.13789   -0.39438

H23   0.60596   -0.01311   -0.44167

H24   0.72902    0.29816   -0.48253

H25   0.80589   -0.03518   -0.40802

CL1  -0.42735   -0.92106   -0.00103

At this stage, the refined structure was compared to the structure shown on transparency

30 of A. Le Bails talk on trends in SDPD, and it was noticed that the (OH)C(NH2) group

of the refined structure was rotated by 180 with respect to the depicted one. Indeed,

turning the (OH)C(NH2) group by 180 significantly improved the Rwp factor, and after

one step of rigid body Rietveld refinement, lattice energy minimisation and adjustment of

the OH torsion angles a final Rwp factor of 2.15% was obtained (Rw=1.66%). The

corresponding atomic coordinates are presented below.

NAME       X          Y          Z

C1    0.66040    0.12422   -0.39107

C2    0.56103    0.19937   -0.37554

C3    0.46084    0.16846   -0.31900

C4    0.48227    0.07579   -0.26131

C5    0.52133   -0.01644   -0.31387

C6    0.62902    0.01130   -0.37525

C7    0.36966    0.04916   -0.20876

C8    0.29366   -0.03209   -0.22552

C9    0.31567   -0.11177   -0.29736

C10   0.41359   -0.07079   -0.35934

C11   0.18172   -0.04821   -0.17355

C12   0.10422   -0.13973   -0.19782

C13   0.11044   -0.18326   -0.27875

C14   0.19694   -0.13715   -0.34475

C15   0.02189   -0.17756   -0.13731

C16  -0.05019   -0.26283   -0.15643

C17  -0.04325   -0.30772   -0.23617

C18   0.03542   -0.26758   -0.29694

C19   0.20933   -0.20914   -0.42263

C20   0.56051    0.29254   -0.41541

C21   0.81095   -0.01770   -0.27809

C22   0.71765   -0.16355   -0.36357

O1    0.00432   -0.13289   -0.05847

O2    0.15176   -0.03886   -0.37321

O3    0.15017    0.00849   -0.11507

O4    0.34318    0.11461   -0.14261

O5    0.36221    0.21452   -0.31193

O6    0.58327    0.10140   -0.20677

O7    0.75457    0.14346   -0.42925

O8    0.65587    0.32826   -0.45965

N1    0.46572    0.35784   -0.41500

N2    0.74533   -0.04954   -0.35751

H1    0.21521   -0.29231   -0.40687

H2    0.28783   -0.18927   -0.46295

H3    0.12878   -0.19885   -0.46316

H4    0.08932   -0.05138   -0.41518

H5   -0.11447   -0.29351   -0.10915

H6   -0.10352   -0.37334   -0.25114

H7    0.39976    0.10598   -0.09727

H8    0.36867   -0.01992   -0.40665

H9    0.86470    0.05200   -0.29319

H10   0.87105   -0.08193   -0.25995

H11   0.74580   -0.00184   -0.22708

H12   0.79839   -0.20772   -0.34461

H13   0.69354   -0.17988   -0.43008

H14   0.64048   -0.18277   -0.32247

H15   0.72088    0.27963   -0.45540

H16   0.46502    0.42475   -0.44853

H17   0.55797    0.09855   -0.14837

H18   0.03466   -0.30361   -0.36024

H19   0.03762   -0.06457   -0.06170

H20   0.55070   -0.07199   -0.26470

H21   0.35190   -0.18326   -0.26730

H22   0.44877   -0.13808   -0.39541

H23   0.60666   -0.01096   -0.44139

H24   0.38740    0.34826   -0.38386

H25   0.80691   -0.03343   -0.40901

CL1  -0.42807   -0.92052   -0.00195

It has to be pointed out that the right orientation of the (OH)C(NH2) group has been

missed due to the small amount of time spend on the final structure refinement. The

hydroxy group and the amino group carry the same number of electrons and have

comparable  distances to the central carbon atom. Therefore it was an oversight not to

calculate the Rwp factor as a function of the torsion angle of the (OH)C(NH2) group, and

the right orientation could have easily been found. The Monte Carlo / Simulated

annealing run that solved the structure did not find the correct orientation, because the

end temperature was significantly higher than the difference of the Rwp factors of both

orientations. The subsequent low temperature Monte Carlo / Simulated annealing run

missed out the right orientation, because the temperature was not high enough to pass the

barrier between the two conformations on the Rwp hypersurface. This example

demonstrates the power of fully automated and integrated software for structure solution

and refinement, but it also shows the importance of chemical and crystallographic

expertise in applying such software.

5 CPU requirements

The high temperature simulated annealing run was performed on a Silicon graphics O2

workstation with a R5000 processor running at 180 MHz. With the molecular geometry

determined by a MOPAC calculation, the structure solution took a couple of hours.

The low temperature simulated annealing run was carried out on a Silicon graphics

Indigo2 workstation with a R10000 processor running at 195 MHz. The run took several

hours.