SDPDRR-3

Sample 1 – Calcium Tartrate Tetrahydrate

# CIF including the details about the crystal structure determination

data_global

_publ_contact_author_name     'Armel LE BAIL'

_publ_contact_author_address

;

Laboratoire des Oxydes et Fluorures - UMR 6010 CNRS,

Facult\'e des Sciences, Universit\'e du Maine,

Avenue Olivier Messiaen, 72085 Le Mans Cedex 9,

France

;

_publ_contact_author_email     armel.le_bail@univ-lemans.fr

_publ_contact_author_fax     '(33) 2 43 83 35 06'

_publ_contact_author_phone     '(33) 2 43 83 33 47'

#======================================================================

# 3. TITLE AND AUTHOR LIST

_publ_section_title

;

Calcium tartrate tetrahydrate second form in rat urinary stones

;

loop_

_publ_author_name

_publ_author_address

'A. Le Bail'

;

Laboratoire des Oxydes et Fluorures - UMR 6010 CNRS,

Facult\'e des Sciences et Techniques, Universit\'e du Maine,

Avenue Olivier Messiaen, 72085 Le Mans Cedex 9, France

;

'D. Bazin'

;

Laboratoire de Physique des Solides - Bat. 510,

Universit\'e Paris XI, 91045 Orsay, France

;

'M. Daudon'

;

Laboratoire de Biochimie A, AP-HP,

Hopital Necker, 149, rue de S\`evres,

75743 Paris Cedex 15, France

;

'V. Maisonneuve'

;

Laboratoire des Oxydes et Fluorures - UMR 6010 CNRS,

Facult\'e des Sciences et Techniques, Universit\'e du Maine,

Avenue Olivier Messiaen, 72085 Le Mans Cedex 9, France

;

#==========================================================================

# 4. TEXT

_publ_section_abstract

;

The title compound, [Ca(C~'4~H~4~O~6~)].4H~2~O is a new triclinic

centrosymmetric polymorph from rat kidney calculus. The four water

molecules belong to the calcium atom coordination, a square antiprism.

;

_publ_section_comment

;

Large crystals (100-200 microns) were extracted from rat kydney.

The chemical analysis suggested a hydrated calcium tartrate. The

crystal structure determination revealed a new tetrahydrated form.

This is unusual since calcium in human urinary stones is mainly

found included in oxalates (70% of the cases) or phosphates (15%)

(Bazin et al., 2007)

The crystal structure of the previously known form of calcium tartrate

tetrahydrate (frequently growing in bottles of wine) has been

reported four times (Ambady, 1968; Hawthorne at al., 1982; Boese and

Heinemann, 1993, Kaduk, 2007) in the P2~1~2~1~2~1~ space group. The

present second form is 2.4% less dense and centrosymmetrical. The calcium

environment is an almost perfect square antiprism (Fig. 1), the four water

molecules forming one of the squares. By the other square of oxygen atoms,

calcium links the tartrate molecules into infinite chains parallel to

the a axis. The two remaining oxygen atoms (O(5), O(6)) of the tartrate

molecule are involved in inter-chain linkage through hydrogen bonding

in the ac and ab planes together with the water molecules (Fig. 2).

The two polymorphs are quite different. In the first form, the calcium atom

is in a distorted Siamese dodecahedron formed by 2 water molecules and the

six oxygen atoms of the tartrate molecule, the two remaining water molecules

participating only in intermolecular linkage.

;

_publ_section_exptl_refinement

;

Crystals were found systematically twinned, and first resisted to the

characterization attempts. Indexing in a triclinic cell was realized

from powder diffraction data by using the McMaille software (Le Bail, 2004).

The structure was solved from the powder data by direct space

methods using the ESPOIR software (Le Bail, 2001) applied to intensities

extracted by iterating the Rietveld decomposition formula (Le Bail et al.,

1988). The tartrate molecule was rotated and translated together with the

calcium and remaining water oxygen atoms up to find an optimum by a Monte

Carlo process. From these convincing results, more efforts were done with

the data recorded from twinned crystals, producing a final refinement of much

higher quality than from the powder data, this in spite of the relatively

high R factor due to peak overlapping from several twin domains. Refinement

applied full-matrix least-squares methods (Sheldrick, 1997). Hydrogen atoms

were taken from a difference Fourier map and refined isotropically with

geometrical constraints and two common isotropic displacement factor (0.07 A^2^

for Hw and 0.04 A^2^ for the others). A few (35) reflections severely affected

by the twinning were omitted.

;

_publ_section_references

;

Allen, F.H., Johnson, O., Shields, G.P., Smith, B.R. & Towler, M. (2004).

J. Appl. Cryst. 37, 335-338.

Ambady, G.K. (1968). Acta Cryst. B58, 380-388.

Bazin, D., Chevallier, P., Matzen, G., Jungers, P. & Daudon, M (2007)

Urol. Res. 35, 179-184.

Boese, R. & Heinemann, O. (1993). Z. Kristallogr. 205, 348-349.

Brandenburg, K. (2001) DIAMOND. Version 2.1e. Crystal Impact GbR, Bonn,

Germany.

Farrugia, L.J. (1997). J. Appl. Cryst. 30, 565.

Hawthorne, F. C., Borys, I. & Ferguson, R. B. (1982). Acta Cryst. B38,

2461-2463.

Kaduk, J. A. (2007). Powder Diffraction 22, 74-82.

Le Bail, A. (2001). Mat. Sci. Forum, 378-381, 65-70.

Le Bail, A. (2004). Powder Diffraction 19, 249-254.

Le Bail, A., Duroy, H. & Fourquet, J. L. (1988). Mat. Res. Bull. 23,

447-452.

Sheldrick, G. M. (1997). SHELXL97. University of Gottingen, Germany.

Stoe & Cie (1998). Stadi4 (Version 1.07) and XRED32 (Version 1.10).

Stoe & Cie, Darmstadt, Germany.

;

_publ_section_figure_captions

;

Figure 1.

ORTEP (Farrugia, 1997) views of tartrate molecule and of the calcium

square antiprism.

Figure 2.

Packing diagram with hydrogen bonds.

;

#===========================================================================

data_I

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

Calcium tartrate tetrahydrate

;

_chemical_name_common  'Calcium tartrate tetrahydrate'

_chemical_melting_point           ?

_chemical_formula_moiety  'C4 H12 Ca O10'

_chemical_formula_sum     'C4 H12 Ca O10'

_chemical_formula_weight          260.22

_symmetry_cell_setting            triclinic

_symmetry_space_group_name_H-M    'P -1'

_symmetry_space_group_name_Hall   '-P 1'

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, -y, -z'

_cell_length_a                    6.241(2)

_cell_length_b                    8.214(3)

_cell_length_c                    10.411(5)

_cell_angle_alpha                 94.92(4)

_cell_angle_beta                  106.00(5)

_cell_angle_gamma                 107.55(3)

_cell_volume                      480.8(4)

_cell_formula_units_Z             2

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     27

_cell_measurement_theta_min       2

_cell_measurement_theta_max       27.55

_exptl_crystal_description        'parallelepiped'

_exptl_crystal_colour             white

_exptl_crystal_size_max           0.115

_exptl_crystal_size_mid           0.095

_exptl_crystal_size_min           0.029

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     1.797

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              272

_exptl_absorpt_coefficient_mu     0.694

_exptl_absorpt_correction_type    none

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71069

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type  'Siemens AED2 diffractometer'

_diffrn_measurement_method     '2\q/\w scans'

_diffrn_detector_area_resol_mean  ?

_diffrn_standards_number          3

_diffrn_standards_interval_count  ?

_diffrn_standards_interval_time   120

_diffrn_standards_decay_%         15

_diffrn_reflns_number             2222

_diffrn_reflns_av_R_equivalents   0.0226

_diffrn_reflns_av_sigmaI/netI     0.0572

_diffrn_reflns_limit_h_min        -8

_diffrn_reflns_limit_h_max        7

_diffrn_reflns_limit_k_min        -10

_diffrn_reflns_limit_k_max        10

_diffrn_reflns_limit_l_min        0

_diffrn_reflns_limit_l_max        13

_diffrn_reflns_theta_min          2.07

_diffrn_reflns_theta_max          27.55

_reflns_number_total              2222

_reflns_number_gt                 1495

_reflns_threshold_expression      >2sigma(I)

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'Ca'  'Ca'   0.2030   0.3060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'C'  'C'   0.0033   0.0016

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_computing_data_collection     'Stadi4 (Stoe, 1998)'

_computing_cell_refinement     'Stadi4'

_computing_data_reduction     'XRED32 (Stoe, 1998)'

_computing_structure_solution     'ESPOIR (Le Bail, 2001)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     'DIAMOND (Brandenburg, 2001)'

_computing_publication_material     'ENCIFER (Allen et al. (2004)'

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.0918P)^2^+1.4964P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          2144

_refine_ls_number_parameters      174

_refine_ls_number_restraints      16

_refine_ls_R_factor_all           0.1122

_refine_ls_R_factor_gt            0.0647

_refine_ls_wR_factor_ref          0.1874

_refine_ls_wR_factor_gt           0.1655

_refine_ls_goodness_of_fit_ref    1.055

_refine_ls_restrained_S_all       1.051

_refine_ls_shift/su_max           0.001

_refine_ls_shift/su_mean          0.000

_diffrn_measured_fraction_theta_max    0.965

_diffrn_reflns_theta_full              27.55

_diffrn_measured_fraction_theta_full   0.965

_refine_diff_density_max    0.973

_refine_diff_density_min   -0.562

_refine_diff_density_rms    0.128

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Ca1 Ca 0.65960(16) 0.80994(12) 0.72621(10) 0.0191(3) Uani 1 1 d . . .

O1 O 0.3163(6) 0.9767(4) 1.0927(3) 0.0232(7) Uani 1 1 d . . .

O2 O 1.1726(6) 0.9733(5) 1.3928(4) 0.0273(8) Uani 1 1 d . . .

O3 O 0.9111(6) 1.0269(4) 1.1676(3) 0.0223(7) Uani 1 1 d D . .

O4 O 0.6207(6) 1.0217(4) 1.3327(3) 0.0217(7) Uani 1 1 d D . .

O5 O 0.9267(7) 0.7075(5) 1.3736(4) 0.0301(8) Uani 1 1 d . . .

O6 O 0.2977(6) 0.7032(5) 1.0343(4) 0.0260(8) Uani 1 1 d . . .

C1 C 0.9834(8) 0.8492(6) 1.3352(5) 0.0186(9) Uani 1 1 d . . .

C2 C 0.3817(8) 0.8494(6) 1.1127(5) 0.0194(9) Uani 1 1 d . . .

C3 C 0.8071(8) 0.8711(6) 1.2081(4) 0.0166(9) Uani 1 1 d D . .

C4 C 0.5809(8) 0.8668(6) 1.2429(5) 0.0182(9) Uani 1 1 d D . .

OW1 O 0.3993(6) 0.6866(5) 0.4955(4) 0.0312(9) Uani 1 1 d D . .

OW2 O 0.8583(6) 0.6536(5) 0.6164(4) 0.0285(8) Uani 1 1 d D . .

OW3 O 0.3111(7) 0.6239(5) 0.7705(4) 0.0296(8) Uani 1 1 d D . .

OW4 O 0.8104(7) 0.6476(5) 0.8984(4) 0.0350(9) Uani 1 1 d D . .

H1W1 H 0.314(12) 0.576(4) 0.460(8) 0.074(10) Uiso 1 1 d D . .

H2W1 H 0.317(12) 0.756(8) 0.502(9) 0.074(10) Uiso 1 1 d D . .

H1W2 H 0.882(13) 0.693(11) 0.542(5) 0.074(10) Uiso 1 1 d D . .

H2W2 H 0.994(9) 0.673(11) 0.683(5) 0.074(10) Uiso 1 1 d D . .

H1W3 H 0.321(15) 0.653(9) 0.857(4) 0.074(10) Uiso 1 1 d D . .

H2W3 H 0.242(13) 0.506(4) 0.745(7) 0.074(10) Uiso 1 1 d D . .

H1W4 H 0.967(5) 0.668(10) 0.932(8) 0.074(10) Uiso 1 1 d D . .

H2W4 H 0.732(11) 0.538(5) 0.905(9) 0.074(10) Uiso 1 1 d D . .

HC3 H 0.781(8) 0.790(5) 1.135(4) 0.036(6) Uiso 1 1 d D . .

HC4 H 0.534(8) 0.790(5) 1.293(4) 0.036(6) Uiso 1 1 d D . .

HO4 H 0.669(8) 0.997(6) 1.414(3) 0.036(6) Uiso 1 1 d D . .

HO3 H 0.822(7) 1.015(6) 1.084(3) 0.036(6) Uiso 1 1 d D . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Ca1 0.0153(4) 0.0188(5) 0.0208(5) 0.0036(3) 0.0030(3) 0.0052(3)

O1 0.0248(17) 0.0240(17) 0.0187(17) 0.0025(13) -0.0011(13) 0.0131(14)

O2 0.0172(17) 0.0295(19) 0.0267(19) 0.0113(15) -0.0011(14) 0.0019(14)

O3 0.0155(16) 0.0246(17) 0.0221(18) 0.0120(14) 0.0020(13) 0.0019(13)

O4 0.0228(17) 0.0256(17) 0.0179(17) 0.0018(14) 0.0043(14) 0.0123(14)

O5 0.033(2) 0.0243(18) 0.031(2) 0.0095(15) 0.0042(16) 0.0114(15)

O6 0.0213(17) 0.0220(17) 0.0255(19) -0.0043(14) -0.0003(14) 0.0037(14)

C1 0.016(2) 0.024(2) 0.016(2) 0.0011(18) 0.0026(17) 0.0100(17)

C2 0.0121(19) 0.023(2) 0.020(2) 0.0050(18) 0.0027(17) 0.0024(17)

C3 0.017(2) 0.019(2) 0.011(2) -0.0001(16) 0.0004(16) 0.0061(17)

C4 0.015(2) 0.018(2) 0.021(2) 0.0055(18) 0.0031(17) 0.0061(17)

OW1 0.0249(19) 0.033(2) 0.029(2) -0.0030(17) -0.0040(15) 0.0126(16)

OW2 0.0233(18) 0.034(2) 0.028(2) 0.0079(16) 0.0037(15) 0.0133(16)

OW3 0.0300(19) 0.0250(18) 0.027(2) 0.0016(15) 0.0077(16) 0.0018(15)

OW4 0.0238(19) 0.035(2) 0.040(2) 0.0178(18) 0.0005(17) 0.0067(16)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Ca1 O1 2.401(4) 2_677 Y

Ca1 O2 2.403(4) 2_777 Y

Ca1 OW1 2.424(4) . Y

Ca1 OW3 2.439(4) . Y

Ca1 OW2 2.447(4) . Y

Ca1 OW4 2.472(4) . Y

Ca1 O3 2.479(4) 2_777 Y

Ca1 O4 2.522(3) 2_677 Y

O1 C2 1.245(6) . Y

O1 O6 2.236(5) . Y

O1 O4 2.606(5) . ?

O1 O3 2.683(5) 2_677 ?

O1 O3 2.972(5) 1_455 ?

O2 C1 1.254(6) . Y

O2 O5 2.213(5) . Y

O2 O3 2.619(5) . ?

O2 O4 2.783(5) 2_778 ?

O2 O4 2.951(5) 1_655 ?

O2 OW1 3.086(6) 2_777 ?

O2 OW2 3.137(5) 2_777 ?

O2 OW1 3.209(5) 1_656 ?

O3 C3 1.407(6) . Y

O3 C1 2.404(6) . ?

O3 C4 2.455(6) . ?

O3 O1 2.683(5) 2_677 ?

O3 O4 2.815(5) . ?

O3 OW4 2.969(5) 2_777 ?

O3 O1 2.972(5) 1_655 ?

O3 OW2 2.991(6) 2_777 ?

O3 HC3 1.83(4) . ?

O3 HO3 0.87(3) . ?

O4 C4 1.426(6) . Y

O4 C2 2.400(6) . ?

O4 C3 2.447(6) . ?

O4 O2 2.783(5) 2_778 ?

O4 OW1 2.919(5) 2_677 ?

O4 O2 2.951(5) 1_455 ?

O4 OW3 3.138(5) 2_677 ?

O4 HC4 1.79(4) . ?

O4 HO4 0.88(3) . ?

O5 C1 1.245(6) . Y

O5 C3 2.372(6) . ?

O5 OW2 2.728(6) 1_556 ?

O5 OW3 2.738(6) 2_667 ?

O5 OW1 2.936(5) 1_656 ?

O6 C2 1.265(6) . Y

O6 C4 2.365(6) . ?

O6 OW3 2.798(5) . ?

O6 OW4 2.853(5) 1_455 ?

O6 OW4 2.947(5) 2_667 ?

O6 H1W3 1.91(3) . ?

C1 C3 1.533(6) . Y

C2 C4 1.527(6) . Y

C3 C4 1.542(6) . Y

C3 HC3 0.91(3) . ?

C4 HC4 0.88(3) . ?

OW1 OW2 2.729(6) 2_666 ?

OW1 OW2 2.899(5) . ?

OW1 O4 2.919(5) 2_677 ?

OW1 O5 2.936(5) 1_454 ?

OW1 O2 3.086(5) 2_777 ?

OW1 OW3 3.116(6) . ?

OW1 O2 3.209(5) 1_454 ?

OW1 H1W1 0.89(8) . ?

OW1 H2W1 0.89(8) . ?

OW2 O5 2.728(6) 1_554 ?

OW2 OW1 2.729(6) 2_666 ?

OW2 OW3 2.933(5) 1_655 ?

OW2 O3 2.991(6) 2_777 ?

OW2 OW4 3.035(6) . ?

OW2 O2 3.137(5) 2_777 ?

OW2 H1W2 0.90(7) . ?

OW2 H2W2 0.89(3) . ?

OW3 O5 2.738(6) 2_667 ?

OW3 O6 2.798(6) . ?

OW3 OW2 2.933(5) 1_455 ?

OW3 OW4 2.971(6) . ?

OW3 O4 3.138(5) 2_677 ?

OW3 H1W3 0.90(3) . ?

OW3 H2W3 0.91(3) . ?

OW4 O6 2.853(5) 1_655 ?

OW4 O6 2.947(5) 2_667 ?

OW4 O3 2.969(5) 2_777 ?

OW4 H1W4 0.90(3) . ?

OW4 H2W4 0.90(3) . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O1 Ca1 O2 92.85(14) 2_677 2_777 ?

O1 Ca1 OW1 135.84(13) 2_677 . ?

O2 Ca1 OW1 79.50(14) 2_777 . ?

O1 Ca1 OW3 86.36(14) 2_677 . ?

O2 Ca1 OW3 149.10(13) 2_777 . ?

OW1 Ca1 OW3 79.72(15) . . ?

O1 Ca1 OW2 148.98(13) 2_677 . ?

O2 Ca1 OW2 80.60(14) 2_777 . ?

OW1 Ca1 OW2 73.07(13) . . ?

OW3 Ca1 OW2 114.51(14) . . ?

O1 Ca1 OW4 88.75(14) 2_677 . ?

O2 Ca1 OW4 136.45(13) 2_777 . ?

OW1 Ca1 OW4 126.24(15) . . ?

OW3 Ca1 OW4 74.44(14) . . ?

OW2 Ca1 OW4 76.18(15) . . ?

O1 Ca1 O3 75.02(13) 2_677 2_777 ?

O2 Ca1 O3 64.86(12) 2_777 2_777 ?

OW1 Ca1 O3 135.03(14) . 2_777 ?

OW3 Ca1 O3 143.17(13) . 2_777 ?

OW2 Ca1 O3 74.77(13) . 2_777 ?

OW4 Ca1 O3 73.68(13) . 2_777 ?

O1 Ca1 O4 63.86(12) 2_677 2_677 ?

O2 Ca1 O4 73.58(12) 2_777 2_677 ?

OW1 Ca1 O4 72.32(13) . 2_677 ?

OW3 Ca1 O4 78.46(13) . 2_677 ?

OW2 Ca1 O4 139.80(12) . 2_677 ?

OW4 Ca1 O4 142.46(14) . 2_677 ?

O3 Ca1 O4 118.64(13) 2_777 2_677 ?

loop_

_geom_hbond_atom_site_label_D

_geom_hbond_atom_site_label_H

_geom_hbond_atom_site_label_A

_geom_hbond_site_symmetry_A

_geom_hbond_distance_DH

_geom_hbond_distance_HA

_geom_hbond_distance_DA

_geom_hbond_angle_DHA

OW1 H1W1 OW2 2_666 0.89(4) 1.84(5) 2.729(6) 178

OW1 H2W1 O4 2_677 0.89(8) 2.26(8) 2.919(5) 131

OW2 H1W2 O5 1_554 0.90(7) 1.86(6) 2.728(6) 163

OW2 H2W2 OW3 1_655 0.89(6) 2.11(6) 2.933(5) 152

OW3 H1W3 O6 1.555 0.89(5) 1.91(5) 2.798(6) 173

OW3 H2W3 O5 2_667 0.91(4) 1.87(5) 2.738(6) 157

OW4 H1W4 O6 1_655 0.90(5) 1.96(6) 2.853(5) 170

OW4 H2W4 O6 2_667 0.90(5) 2.10(5) 2.947(5) 155

O4 HO4 O2 2_778 0.88(3) 1.94(3) 2.783(5) 160

O3 HO3 O1 2_677 0.87(3) 1.82(3) 2.683(5) 169