SDPDRR-3

Sample 2 - La18W10O57

# Crystal Structure Determination

In a previous study [1] (from single crystal data though the structure determination was not completed because it was not possible to obtain good crystals), the commonest six-layered polytype was said to belong to the space group P63/mmc (no piezoeffect detected) with cell parameters a = 9.04(1) Å and c  = 32.60 – 33.65 Å depending on the composition of the crystal. This cell is confirmed here by a satisfying whole powder pattern fit (WPPF) by using the Le Bail method [2] through the Fullprof software [3]. The extracted intensities from the synchrotron powder pattern were then used for attempting the structure solution by direct space methods as embedded in the ESPOIR software [4], searching for the heavy W and La independent atoms by a Monte Carlo process. Nothing better than Rp > 35% could be obtained during various tests in the P63/mmc or P63mc space groups. Direct or Patterson methods failed as well to provide a satisfying starting model. Then the search for a solution was made in the c/6 subcell, in spite of the fact that very intense reflections had to be excluded (scaling the most intense 206 at I = 100, the 207 is at I = 13, the 217 is at I = 14), trying various space groups without extinction, a promising model leading to Rp = 22% on 220 remaining peaks was finally obtained from the ESPOIR software in the P-62m space group, corresponding to a La/W = 2 ratio (La2WO6 formula). No extension of that model in the large cell could be obtained in the P63/mmc or P63mc space groups. Then the other space groups compatible with the hh2-hl, l=2n reflection condition were examined (P-62c, P-31c, P31c). The small initial model could be extended in the large cell by using the acentric space groups, for instance with 4 La and 5 W independent atom sites in the general or special positions of P-62c. Using that estimation of the number of independent sites, ESPOIR provided new starting coordinates for the La and W atoms in the large cell, decreasing Rp to a satisfying 23%. Introducing these atomic coordinates into a Rietveld [5] refinement led then to RB = 19.7 and RF = 11.1 % when the thermal parameters were refined (most having negative values because of the absence of absorption correction at this stage). From a Fourier difference map, an additional W atom site was detected as well as all the oxygen atoms in ten independent sites. Further refinements suggested that this new W site had to be half occupied, leading to the La18W10O57 formula with Z = 2. A part of the W atoms were found in octahedral coordination but the majority of them are in a unusual trigonal prismatic coordination. We then tried to confirm that by a new search for the oxygen atom position from the neutron data by using the ESPOIR software, fixing the La and W atoms to the positions obtained from the synchrotron data refinements. The same model was built up by ESPOIR from the neutron data. This unusual trigonal prismatic coordination was previously observed for the WO6 group in the X-ray studies of Pr3WO6Cl3 [6] and La3WO6Cl3 [7], the latter structure being then confirmed from neutron powder diffraction data [8]. Indeed, the cell parameters of these halotungstates are similar to the c/6 subcell with a = 9.4048 and c = 5.4253 (S.G. P63/m), to be compared to a = 9.0443, c/6  = 5.4471 for the title compound. A comparison of the La and W atom coordinates in both compounds is provided in Table 1. The W atom in La3WO6Cl3 is at z = ¼ and ¾ whereas the corresponding W2 in the subcell of the title compound is exclusively at z =1/2 and there is an additional W1 at 0,0,0. This explains why early attempts to solve the La18W10O57 structure by building a model from the La3WO6Cl3 structure failed.

Tests in order to see if reducing the symmetry would allow the half occupied W site to become fully ordered were made in P31c and in various subgroups of P-62c and P31c (Ama2, Cc) with no convincing result : the number of atomic coordinates to be refined becomes prohibitive. From the low-resolution powder pattern, it was hardly possible to refine all thermal parameters independently. The details of the Rietveld refinements, the atomic coordinates and the interatomic distances and angles are gathered respectively in Tables 2, 3 and 4.  The W4 atom which has half of the times W6 as a neighbour is the only tungsten atom presenting a high thermal parameter (from the synchrotron data refinement). It is clear that according to the presence of W6 or not, then the W4 position will be modified along z. Accordingly, the very short W4-W6 interactomic distance (2.42 Å) should be considered cautiously. These two WO6 octahedra sharing a face are also a very unusual feature of the title compound. See the Rietveld plots below, and the drawings of the projections along [001] and [110] of the crystal structures of La18W10O57 and La3WO6Cl3.

The neutron data fit is under the expected quality with Rp = 12.9 %. This is due to inhomogeneities in the sample which could not be prepared in large quantity without some composition variation. In spite of this problem, the atomic coordinates from the synchrotron and neutron fits compare well. Anyway, the current description of that structure, having resisted up to now to characterization attempts, is the best we can do with these data and samples.

# References

[1] V.K. Yanovskii and V.I. Voronkova, Crystallography and properties of lanthanum oxytungstate, La2WO6, Sov. Phys. Crystallogr., 20 (1975) 354-355.

[2] A. Le Bail, H. Duroy and J.L. Fourquet, Ab initio structure determination of LiSbWO6 by X-Ray powder diffraction, Mat. Res. Bull. 23, 447-452 (1988).

[3] J. Rodriguez-Carvajal, Recent advances in magnetic-structure determination by neutron powder diffraction, Physica B, 192 (1993) 55-69.

[4] A. Le Bail, ESPOIR : A program for solving structures by Monte Carlo from powder diffraction data, Mat. Sci. Forum, 378-381 (2001) 65-70.

[5] H.M. Rietveld, A profile refinement method for nuclear and magnetic structures, J. Appl. Crystallogr. 2 (1969) 65-71.

[6] T.M. Polyanskaya, Dokl. Akad. Nauk SSR 187 (1969) 1043.

[7] L.H. Brixner, H.Y. Chen and C.M. Foris, Structure and luminescence of some rare earth halotungstates of the type Ln3WO6Cl3, J. Solid State Chem., 44 (1982) 99-107.

[8] J.B. Parise and L.H. Brixner, Refinement of the structure of trilanthanum trichlorohexaoxotungstate, La3WO6Cl3 from neutron powder diffraction data, Acta Cryst., C39 (1983) 1326-1328.

Table 1

Initial model for La18W10O57 in the c/6 subcell in the P-62m space

Group, compared to the W and La positions in the La3WO6Cl3 structure

described in the P63/m space group.

Atom  Wyckoff	x		y		z

Position

c/6 subcell of La18W10O57

W1       1a       	0		0		0

W2       2d       	1/3		2/3		1/2

La1	  3f		0.429		0		0

La2	  3g		0.743		0		1/2

La3WO6Cl3

W	   2c		1/3		2/3		1/4

La	   6h		0.0906		0.6865		3/4

Table 2

Rietveld refinements with the Fullprof program

Synchrotron			Neutron

Wavelength (Å)			0.60044			1.5944

Absorption correction		muR-eff = 4.95		none

Space group					P-62c  (No 190)

Cell parameters	a(Å)		9.04428(4)			9.0518(2)

c(Å)		32.6829(1)			32.708(1)

Volume				2315.26(2)			2320.9(1)

No of fitted parameters		89				70

No of background parameters	25				14

No of reflections			1086				943

Zeropoint (°)			0.0012(2)			0.168(3)

Eta (Pseudo-Voigt)		0.574(12)			0.53(2)

Halfwidth parameters	U	0.00241(6)			0.102(6)

V	0				-.26(1)

W	0.000150(1)			0.299(8)

Average FWHM			0.0193			0.441

Asymmetry parameters		0.035(3)			0.089(9)

0.0080(3)			0.026(4)

X parameters			0.0011(6)			0

Reliability factors for points with Bragg contribution

N-P+C					13417				2749

R-factors (not corrected for background)

Rp			7.03				5.91

Rwp			9.44				7.71

Rexp			9.52				1.41

Chi2			0.983				29.8

Conventional Rietveld R-factors

Rp			17.9				12.9

Rwp			17.6				15.1

Rexp			17.8				2.76

Chi2			0.983    			29.8

Bragg R-factors

RB			5.91				6.45

RF			4.93				3.87

Table 3.

Atomic coordinates in the P-62c space group from X-ray synchrotron and neutron data.

Atom  Wyckoff 	        x 		       y		       z 	    	   B

position

La1   12i	X	0.6151(3)	0.0401(3)	0.58377(8)	1.40(4)

N	0.6174(10)	0.0416(9)	0.5826(2)	0.88(6)

La2   12i	X	0.2776(2)	0.0367(2)	0.33203(7)	0.82(3)

N	0.2747(9)	0.0308(8)	0.3305(3)	0.88(6)

La3   6h	X	0.3704(4)	0.4291(5)	1/4		1.07(5)

N	0.3728(15)	0.4276(16)  1/4		0.88(6)

La4   6g	X	0.2567(4)	0		0		1.19(6)

N	0.2570(14)	0		0		0.88(6)

W1	4e	X	0		0		0.58496(8)	0.91(4)

N	0		0		0.5873(8)	0.76(12)

W2	4f	X	1/3		2/3		0.33313(7)	0.87(3)

N	1/3		2/3		0.3335(9)	0.76(12)

W3    4f	X	1/3		2/3		0.00314(5)	0.82(4)

N	1/3		2/3		0.0032(6)	0.76(12)

W4    4f	X	1/3		2/3		0.63634(8)	2.50(5)

N	1/3		2/3		0.6384(6)	0.76(12)

W5    2b	X	0		0		1/4		0.73(6)

N	0		0		1/4		0.76(12)

W6*	4f	X	1/3		2/3		0.7186(1)	0.92(7)

N	1/3		2/3		0.7123(14)	0.76(12)

O1	12i	X	0.8309(33)	0.9826(33)	0.2130(7)	0.97(10)

N	0.8334(17)	0.9872(15)	0.2137(3)	1.02(4)

O2	12i	X	0.9759(33)	0.8256(31)	0.6204(8)	0.97(10)

N	0.9763(17)	0.8256(19)	0.6212(3)	1.02(4)

O3	12i	X	0.6869(38)	0.5043(32)	0.7069(6)	0.97(10)

N	0.6975(16)	0.5126(16)	0.7047(3)	1.02(4)

O4	12i	X	0.5216(28)	0.7090(30)	0.0445(6)	0.97(10)

N	0.5147(15)	0.7051(17)	0.0454(3)	1.02(4)

O5	12i	X	0.6834(32)	0.4980(27)	0.6314(6)	0.97(10)

N	0.6751(13)	0.5010(13)	0.6298(3)	1.02(4)

O6	12i	X	0.1509(32)	0.1829(31)	0.5456(7)	0.97(10)

N	0.1578(15)	0.1811(17)	0.5444(3)	1.02(4)

O7	12i	X	0.4758(29)	0.1799(29)	0.3932(6)	0.97(10)

N	0.4718(15)	0.1848(14)	0.3908(3)	1.02(4)

O8	12i	X	0.1392(24)	0.6003(26)	0.9718(6)	0.97(10)

N	0.1425(14)	0.5995(12)	0.9777(3)	1.02(4)

O9	12i	X	0.5176(23)	0.3720(26)	0.3246(6)	0.97(10)

N	0.5137(13)	0.3672(13)	0.3241(3)	1.02(4)

O10	6h	X	0.4628(38)	0.1699(39)	1/4		0.97(10)

N	0.4678(20)	0.1767(20)	1/4		1.02(4)

* half occupied site

Table 4

Selected interatomic distances (La-O < 3.2 A) and angles (from neutron data)

La1-O4  2.403(13)   La2-O3  2.386(18)   La3-O1 x2  2.498(14)   La4-O6 x2  2.367(13)

-O5  2.501(16)      -O1  2.479(18)      -O3 x2  2.51(2)        -O4 x2  2.426(16)

-O6  2.511(18)      -05  2.485(17)      -O3 x2  2.583(15)      -O6 x2  2.660(13)

-O4  2.517(19)      -O7  2.555(13)      -O10    2.70(2)        -O8 x2  2.794(16)

-O8  2.521(11)      -O1  2.558(13)      -O10    2.80(3)

-O2  2.523(19)      -O2  2.574(15)      -O9 x2  2.915(15)

-O5  2.772(12)      -O2  2.63(2)

-O7  2.788(12)      -O9  2.722(11)

-O7  2.803(15)      -O9  2.873(14)

-010 3.071(11)

Trigonal prisms

W1-O2 x3  1.85(2)   O2-W1-O2  87.8(13)   O2-W1-O6 144.5(14)   O2-W1-O6 124.5(15)

W1-O6 x3  2.09(2)   O6-W1-O1  79.7(10)   O2-W1-O6  80.1(11)

W2-O5 x3  1.91(1)   O3-W2-O3  83.5(11)   O3-W2-O5 139.4(12)   O3-W2-O5 129.7(14)

W2-O3 x3  1.95(2)   O5-W2-O5  84.6(11)   O3-W2-O5  79.0(11)

W5-O1 x6  1.877(10) O1-W5-O1  84.2(12)   O1-W5-O1  78.5(8)    O1-W5-O1 134.4(11)

Octahedra

W3-O8 x3  1.732(13)  O4-W3-O4  79.1(12)   O4-W3-O8  85.6(10)   O4-W3-O8  95.3(11)

W3-O4 x3  2.037(17)  O8-W3-O8  98.7(13)   O4-W3-O8 164.5(13)

W4-O7 x3  1.860(14)  O7-W4-O7  96.0(11)   O7-W4-O9  86.9(9)    O7-W4-O9  90.8(10)

W4-O9 x3  1.985(15)  O9-W4-O9  85.8(11)   O7-W4-O9 172.2(10)

W6-O9 x3  1.96(3)    O9-W6-O9   86.9(15)  O9-W6-O10  91.7(13)  O9-W6-O10  93.7(13)

W6-O10 x3 2.05(3)    O10-W6-O10 87.7(16)  O9-W6-O10 178.4(18)

W-W short distances

W6-W4  2.42(5)       W6-W6  2.46(6)