## Slide 1
Reverse Monte Carlo and Rietveld modelling of BaMn(Fe,V)F7 glass structures from neutron data _____ A. Le Bail Université du Maine – France alb@cristal.org - http://www.cristal.org/

## Slide 2
Content
- Introduction
- Experimental
- Models ?
- RDM modelling
- RMC modelling from enlarged RDM models
RMC modelling from random starting models
Conclusions on BaMn(Fe/V)F7 glasses

## Slide 3
Introduction
Structure simulations by the reverse Monte Carlo (RMC) method applied to starting models built up from enlarged crystal structures, selected from the quality level of a Rietveld fit of their scattering data, were reported for glassy SiO2, ZnCl2, and NaPb(Fe,V)2F9.
The Rietveld for disordered materials (RDM) method has previously shown its potentiality to reveal very fast (quite small computing time) if a given crystalline model would be a good starting point for further large-scale modelling by RMC.
This approach is used here for modelling the structure of fluoride glasses for a composition BaMn(Fe,V)F7 selected because it corresponds to the existence of a large number of known different crystal structures, and because of the quasi-isomorphous Fe/V substitution in fluoride materials.

## Slide 4
Experimental
- Neutron data recorded on instrument D4 (ILL –Grenoble)
 = 0.497 Å
Density number for the two glasses :
0 = 0.0710  0.0003 atom.Å-3

## Slide 5
Seven crystal structure-types are known with that composition :
- BaMnFeF7 (I)
- BaMnGaF7 (II)
- BaZnFeF7 (III)
- BaCaGaF7 (IV)
- BaCuFeF7 (V)
- BaCuInF7 (VI)
- BaNaZrF7 (VII)
Models ?
The BaMn(Fe,V)F7 glasses crystallize in type (II)

## Slide 6
Model (I) : BaMnFeF7
Three-dimensional octahedral lattice with edge-sharing dinuclear Mn2F10 units (green) linked by corners to FeF6 octahedra (blue).
A glass with BaMnFeF7 composition does not crystallize in type I.

## Slide 7
Model (II) : BaMnGaF7
Edge sharing of GaF6 octahedra (green) and MnF8 (red) polyhedra occur, forming dinuclear M2F12 units interconnected by corners to MnF6 octahedra (blue) and other M2F12 units, building disconnected layers.
Why glasses prefer to crystallize in this layered structure-type rather than into a 3D network of corner-sharing octahedra ?

## Slide 8
Model (III) : HT-BaZnFeF7
3D structure with edge sharing of ZnF6 and FeF6 octahedra, forming M2F10 groups interlinked by corners, like in type I but differently organized.

## Slide 9
Model (IV) : BaCaGaF7
GaF6 octahedra (green) and CaF8 square antiprisms (red) are linked by corners and edges forming a two dimensional structure.
Ga3+ and Fe3+ ionic radii are similar, the difference between Ca2+ and Mn2+ (smaller) is not a problem since MnF8 square antiprisms are existing in other structures (type II for instance).

## Slide 10
Model (V) : BaCuFeF7
Edge sharing dioctahedral groups CuFeF10 connected by corners in a 3D array, related to HT-BaZnFeF7 (type III).
Partial cationic disorder.

## Slide 11
Model (VI) : BaCuInF7
The 3D structure is built up from infinite rutile-like chains of edge-sharing octahedra, interconnected by octahedra corners.
Cu and In are disordered.

## Slide 12
Model (VII) : BaNaZrF7
3D structure build up from infinite zig-zag cis-chains of edge sharing NaF8 cubes (blue) linked together by ZrF7 monocapped trigonal prism (green).
Systematic microtwinning.

## Slide 13
Fe/V Isomorphous substitution
As a rule, when a Fe3+-based crystalline fluoride exists, the isostructural equivalent V3+ material can be prepared too, with generally no more than 1% variation in cell dimensions.
Neutron Fermi scattering lengths : Fe : 0.954 V : -0.038 The substitution ensures a quite large contrast

## Slide 14
RDM modelling – What is it ?
Done by using the ARITVE software which is simply a Rietveld method program allowing :
a huge limit of reflection number (60000 on each pattern)
3 interference functions maximum fitted simultaneously
a huge limit of reflections overlapping at the same angle (20000)
a small number of parameters to be refined (max = 75)
only Gaussian peak shape
line broadening following a Caglioti law (size/microstrain)
= RDM : Rietveld for Disordered Materials

## Slide 15
RDM performance compared to RMC ?

## Slide 16
RDM results on BaMn(Fe/V)F7 glasses
The fit quality by the Rietveld method is characterized by a profile reliability factor :
Rp = 100*|Iobs-kIcalc|/|Iobs| (%)
The reliability factors were calculated for two fit ranges, full range (Rp1), and low angle-limited range (Rp2), because the full range includes large-angle data which are rather smooth, tending to produce small Rp values whatever the fit is good or not.
Models I and II provide the smallest  Rp values

## Slide 17
Example of RDM fits for model I : Fe

## Slide 18
Example of RDM fits for model I : V

## Slide 19
RMC modelling from enlarged RDM models
Constraints on coordinations and interatomic distance ranges are applied in order to not destroy the Mn and (Fe,V) polyhedra and their connectivity. Calculations took several days on fast PCs (processor > 2 GHz).
Rp1 (%) for the 0.8-22.2 Q range (Å-1) (Fe and V) and Rp2 for 0.8-9 Å-1.
1.91 < Rp1 < 2.21 % for the Fe-based glass 2.50 < Rp1 < 2.67 % for the V-based glass
ANY MODEL IS OK ??

## Slide 20
Example of RMC+RDM fits for model II : Fe

## Slide 21
Example of RMC+RDM fits for model II : V

## Slide 22
The 4320 atoms in the box – Model II
Green MnF6 polyhedra, blue (Fe,V)F6 polyhedra, Ba atoms as yellow spheres.

## Slide 23
RMC modelling from random starting models
Cubic box of 5000 atoms (cubic edge L = 41.2956 Å).
Very long runs were needed up to obtain the expected sixfold fluorine coordination around the 3d elements.
The "best" of three independent modellings provided Rp1 = 2.11 % (Fe); Rp1 = 2.59 % (V); Rp2 = 4.36 % (Fe); Rp2 = 5.54 % (V).
NOT BETTER THAN THE RMC+RDM MODELS
As previously observed when modelling NaPbFe2F9 glasses, the sixfold polyhedra show all possibilities between octahedra and trigonal prisms.

## Slide 24
The best pure random RMC model : Fe

## Slide 25
The best pure random RMC model : V

## Slide 26
The 5000 atoms in the cubic box
Green MnF6 polyhedra, blue (Fe,V)F6 polyhedra, Ba atoms as yellow spheres.

## Slide 27
Conclusions on BaMn(Fe/V)F7 glasses
Several previous consecutive RDM-RMC modelling have shown that the starting crystalline model leading to the most satisfying structure simulation of a glass is generally that of its crystallization product, when it is a unique phase.
The conclusion of the present study is again favouring a generalization of this observation since the structure-type II is found to represent the most satisfying model which can be built by RMC among the types I-VII. Even the fully random models built by RMC cannot produce a better agreement between the observed and calculated neutron interference functions.
However, there is not a so clear gap in fit quality between model II and some others which would allow to claim having elucidated these fluoride glass structures. As usual, the frustrating conclusion is moderated. And the preference of the glass for crystallizing into the structure-type II rather than into the type I is not well understood.

## Slide 28
This may mean that the availability of only two interference functions for a four-elements glass (for which ten interference functions would have to be known) gives rise to an undetermined problem, in spite of the coordination and distance constraints.
It may also signify that the average orders at short and medium-range which characterizes all these models are finally very similar, in spite of their obvious differences in connectivity and three- or two-dimensionality.
The RDM method operates with a considerably smaller number of degrees of freedom (a few atomic coordinates), and thus produces more clear differences in the fits from various models.
Why not more differences between models ?

## Slide 29
The ARITVE software for RDM
can be downloaded at :
http://www.cristal.org/aritve.html