## Slide 1
McMaille v3: indexing via Monte Carlo search
against an idealized powder profile
A. Le Bail Université du Maine Laboratoire des Fluorures CNRS – UMR 6010 alb@cristal.org http://cristal.org/

## Slide 2
Content
- Introduction : indexing in the powder diffraction maze
The SDPD Round Robin 2002 indexing part – ultra brief report
McMaille (pronounce « MacMy ») short pseudo-demos (screen copies)
« Simplicity » of the Monte Carlo algorithm in McMaille
McMaille v2 : Gaussian profiles
McMaille v3 : Columnar peak shape
About the (accuracy + enlarged peaks) apparent contradiction
« Refinement » and optimization
Indexing multiphase patterns and impurity lines problems
Conclusions

## Slide 3
No way to escape the indexing bottleneck in the SDPD maze
(figure extracted from the IUCr monograph 13)
SDPD = Structure Determination by Powder Diffractometry

## Slide 4
SDPD Round Robin 2 – September 2002 (indexing part)
8 powder patterns to index 100 participants having downloaded the data 6 answers received in due time (1 month)
CRYSFIRE (P1, P3), DICVOL (P2), ITO (P4), Index (P5) and X-Cell (P6).

## Slide 5
Example : sample 3 of the Round Robin in principle very simple : cubic
Organizers: 18.881 18.881 18.881 90 90 90 (vol 6734 Å3)
P1: 13.349 13.349 9.439 90 90 90 (Tetragonal - 1638Å3)
P2: 18.878 18.878 18.878 90 90 90
P3: 13.354 13.354 9.442 90 90 90 (Tetragonal - 1638Å3)
P4: no solution
P5: 18.878 18.878 18.878 90 90 90
P6: 18.88 18.88 18.88 90 90 90
50% successful only !
Possibly because of too small default maximum volume limit. P1 and P3 provide the same (correct) subcell.

## Slide 6
Well, the Round Robin conclusion is that indexing would not be that easy ?
Hence the need for more efforts in the less explored directions for indexing, using not only peak positions but also intensities, and why not the whole powder profile (that way was initiated by Kariuki et al., 1999, applying a genetic algorithm). McMaille follows the same route by using the Monte Carlo method in order to generate randomly cell parameters tested against an idealized powder profile.
Find more details about the SDPD-2002 Round Robin at : Web site : http://sdpd.univ-lemans.fr/sdpdrr2/results/ Report : in the IUCr - CPD – Newsletter N°29 – July 2003

## Slide 7
McMaille short pseudo-demos (screen copies) (live demos were done last Sunday at the powder diffraction workshop)
Program download (GNU Public Licence) :
http://www.cristal.org/McMaille/
Crystallographers want solutions fast ! Is that possible with McMaille ? YES… if you consider 5-15 minutes being fast…
The first recommended approach with McMaille is to use the quite simple automated « black box » mode.
Peak positions and intensities can be extracted by using the WinPlotr program which is able to build the McMaille entry data file directly for the automated mode.

## Slide 8
Start WinPlotr, open the powder pattern file, select « automatic peak search »

## Slide 9
Select appropriate conditions (CuKalpha1/2 doublet), click OK

## Slide 10
WinPlotr will establish a list of peak positions and intensities

## Slide 11
Save the results for McMaille

## Slide 12
Gives few details : a title, the wavelenght, the zeropoint, that’s all !

## Slide 13
The preparation is finished, the file for McMaille is created

## Slide 14
That file looks like quite simple :

## Slide 15
You need then to run McMaille, typing the entry file name :

## Slide 16
What is examined in the automated « black box » mode ?
All symmetries in restricted volumes and cell parameters
(unrestricted in cubic)
Hence the need for exploring other ranges in manual mode if the automated mode was unsuccessful, or if you want to have a deepest look
Fortunately, McMaille produces a file ready for the manual mode at the end of an automatic examination

## Slide 17
The file created for the manual mode :

## Slide 18
Running McMaille with that file in manual mode :

## Slide 19
The fit generated by McMaille for that solution, displayed by WinPlotr (as a .prf file) :

## Slide 20
Now the let us index the SDPDRR-2 samples 1, 2, 3 (synchrotron radiation) in manual mode (the true crystal class is selected, and the volume is explored inside a defined volume range – the correct range… more fast and easy…).

## Slide 21
The corresponding plot :

## Slide 22
Sample 2 :

## Slide 23
The corresponding plot :

## Slide 24
Sample 3 (synchrotron data)

## Slide 25
A more pure sample was used, only one small intensity impurity line visible :

## Slide 26
The CRYSFIRE monoclinic test file in automated mode : how long with McMaille ? < 5 minutes at > 2Ghz. The next release of CRYSFIRE will include McMaille

## Slide 27
The corresponding plot :

## Slide 28
Now let us examine more closely all the McMaille « secrets »

## Slide 29
« Simplicity » of the Monte Carlo algorithm in McMaille

## Slide 30
Saving time with the hkl list
hkl Miller indices are predetermined (400 to 1000) for every crystal system and saved in files read once at the beginning.
They are only selected (not ordered which would be too long) according to the cell parameters trial and cut off at d(hkl)min.
If a calculated profile do not intercept any observed one, then the corresponding hkl set is considered as unobserved, not taken into account.

## Slide 31
McMaille v1 and v2 : Gaussian profiles
Choice was made of an idealized profile (Gaussian shape applied to extracted peak positions) rather than using the raw pattern – for velocity reasons. Fit by 3 iterations of the Rietveld decomposition formula (= Le Bail method).
Version 1 worked only in cubic for studying the feasibility which was quite encouraging with 1000 tests per second by using a > 2GHz processor.
Version 2 extended to all crystal systems, 300 tests per second in triclinic.
Not fast enough with low symmetries needing 108-109 tests…

## Slide 32
McMaille v3 : Columnar peak shape
Speed increased by a factor 20…
20.000 tests per second in cubic, 6000 in triclinic.
No real need for a fit, the observed and calculated columns are given the same height and same width.
The R factor becomes function of the percentage of overlapping between observed and calculated columns.

## Slide 33
SDPDRR2 Sample 3 – conventional X-rays
Peak positions extracted by WinPLOTR

## Slide 34
The columnar peak shapes used by McMaille v3

## Slide 35
Zooming on the last reflections
The width in the automated mode is calculated as : 0.3 x  / 1.54056 it depends on the user in manual mode

## Slide 36
One of the 2 cases leading to « refine » a cell : Ni > N - N’
Ni = 19 N = 20 N’ = 2
R = 98% ! But that cell proposal is retained
A peak is considered as indexed if some overlap occurs with a calculated one. The second case leading to « refine » a cell is when R < R1 (usually 50%).

## Slide 37
About (accuracy + enlarged peaks) apparent contradiction
The more the « observed » columns are large, the more you have chances to intercept them by the calculated columns.
Cubic example : A column at 10°(2) (d = 8.838 Å) will extend from 9.85 to 10.15 °(2) (d =8.972 to d = 8.707;  = 1.54056 Å). So that if the peak is the 200 reflection, the range of a values leading certainly (if the accuracy is high) to the solution is [17.41-17.94 Å]. Any test in that interval larger than 0.5 Å is a winning test.
But at the « refinement » stage, it is mainly the position accuracy which is important. It will lead effectively to low R values (exact overlapping corresponds to R = 0.) allowing to distinguish the true solution from bad proposals.

## Slide 38
More on the cell « refinement » in McMaille
At R < R1 ~ 50%, no least square refinement is possible
So that the cell parameters are adjusted by Monte Carlo (200 steps in cubic to 5000 steps in triclinic) with small amplitude change (|delta max| = 0.02 Å). Similar to tempering ?
The best proposal at R < R3 ~ 5% is finally least-squared refined and classical figures of merit (M20, F20) are calculated.

## Slide 39
Final plot produced by McMaille, displayed by WinPLOTR :
Other software compatible with McMaille outputs : CHEKCELL, CRYSFIRE
with Gaussian peak shapes and width / 2.

## Slide 40
Effects with various Probability values (probability to accept a new cell parameter if the fit is not improved) : number of times the correct answer is found for the same number of Monte Carlo steps :
Optimization : not being trapped in a false minima Accepting a parameter change even if the fit is not improved
P (%) 0 15 30 45 60 75 100
Test 1 – orthorhombic 41 45 32 27 15 6 1 Test 2 – rhombohedral 28 41 40 28 17 10 6 Test 4 – monoclinic 47 60 46 45 25 19 2 Test 6 – triclinic 36 42 36 24 18 12 12
The tendency is to work better with P ~ 15 %, as a mean
P : a value of 15 means that in 15% of the tests, a parameter change may be accepted even if that change does not lead to any R decrease or number of indexed reflections improvement (no change means that you keep the previous parameter unchanged)
P = 100 : always accepted even if it does not improve the fit
P = 0 : not accepted at all if it does not improve the fit

## Slide 41
Relative insensitivity to impurity
The user decides by two control parameters :
N’ : number of unindexed lines.
R2 : consider only proposals with R < R2. Fixing it at 15% means that cell proposals explaining at least 85% of the peaks total intensity will be listed.
An impurity should not concern more than 15% of the total intensity, right ? But the number of (small) peaks belonging to the impurity can be high…

## Slide 42
Preliminary results about impurity lines :
Provided the total intensity of the impurity lines is less than 15% of the total intensity :
With less than 35% (in number) of impurity lines, McMaille generally provides the correct cell in top position. However, the figures of merit decrease.
With 35-50% (in number) of impurity lines, McMaille may still propose the correct cell, but generally not in first position. Thus it is more difficult to locate it.

## Slide 43
Example of an orthorhombic phase indexed in spite of 12 small impurity lines added to 20 (37.5% in number)

## Slide 44
Beyong impurities, indexing multiphase patterns
Multiple synthesis in varying conditions should reveal the multiphase nature of the sample.
It is much better to adjust the synthesis conditions, and even if the phases cannot be prepared as pure phases, intensities variations should allow to define the peaks belonging to one or the other phase.
But if really you want to attempt indexing of a mixture, let us see the cost on the McMaille organization chart…

## Slide 45
Indexing a 2-phases powder pattern with McMaille

## Slide 46
Preliminary conclusions about two-phases indexing with McMaille
Provided at least 30 lines are examined with 13-17 lines belonging to each phases, and 40-60% of the total intensity distributed to each phase, then :
McMaille appears to be able to produce solutions in reasonable times (<1 hour) for combinations of two phases either cubic or hexagonal or tetragonal or orthorhombic.
Monoclinic and triclinic not examined (too long).

## Slide 47
Example of 2-phases indexing (20 minutes) : One mixture of a tetragonal with an orthorhombic phase McMaille combines the cell proposals by couples and detects the best combinations indexing the largest number of peaks :

## Slide 48
Conclusions
- Promising (?) method…
Already quite efficient if you have time and a fast computer.
Needs some skills in manual mode, but nothing to do in « black box » mode (except finding the zeropoint).
Improve it if you have some ideas (GNU Public Licence).
Completely free access.
Use cautiously the 2-phases mode…
A useful address for a distance learning course : SDPD Internet Course http://sdpd.univ-lemans.fr/course/